## Slide 1
Contents
Raw Material
Manufacturing Procedure
A. Material Preparation
B. Door Leaf Process
C. Door Frame Process
D. Painting Process
E. Product Inspection
F. Packaging

## Slide 2
Raw Material

## Slide 3
No. | Material |  | Feature | Application | Picture
1 | Solid wood |  | Natural, environment friendly, shrinkage and swelling | Solid wood door, press line, edge, carved panel | 
2 | Lumber | Fir (hemlock) |  | Composite Door Leaf Core: Fir，light log, stable, economic. Frame Core: Eucalyptus, not easy to deform, can carry heavy door leaf, strong nail-holding ability, etc., high density | 
3 |  | Eucalyptus(hardwood) |  |  | 
4 | MDF |  | Density: 500~800kg/m³, made of wood fiber powder, easy to process, stable performance, smooth, easy to paste veneer and paint | Baseboard for the veneer, modelling panels、base material for the groove | 
Main Material:

## Slide 4
No. | Material | Feature | Application | Picture
5 | Finger joint board | Stable, no deformation | Door leaf outer edge band, architrave base materail | 
6 | Plywood | Thin layers of wood stuck together, stable, non-deformable, strong nail-holding ability | cover plate of door frame, subplate, face plate of door leaf | 
7 | Glue | Chemical composition | Each gluing processing | 
8 | Paint | Paint film hardness, transparency, hand-feeling, leveling, richness | Product surface finish | 
9 | Veneer | 0.45mm，0.3mm veneer stick on non - woven fabric to prevent cracking | Product surface，0.3mm non - woven veneer is mainly used to paste profiled lines | 

## Slide 5
Manufacturing Procedure

## Slide 6
High power central dust removal system
With this system which imported from Europe, the workshop can always be in a clean and tidy environment, which is the premise for creating high quality products.
A. Material Preparation

## Slide 7
Dry Kiln:
Large steam drying, can dry thousands of cubic meters of wood at a time, so that the wood has sufficient health time after drying, and is equipped with a wood sterilization system to protect against insects.

## Slide 8
Wood Carbonizer
It significantly reduces the exchange capacity of the carbonized wood with the external water, thereby greatly reducing the deformation, shrinkage, and swelling due to moisture changes during production. However, due to the wood structure, some materials are prone to bursting and are difficult to carbonize. They are generally dry and non-carbonized, such as cherry, oak, and sapele.

## Slide 9
Electronic Sawing
Core Material Sanding
Full computer operation, higher precision and safer operation than normal manual operation. If the precision of the raw material is not correct, the product can not reach 90° right angle.
The cutting thickness is between 0.3cm and 11cm.

## Slide 10
Sorting
Cutting
Wireless Sewing
Observing the quality through light transmission
Veneer Processing

## Slide 11
B. Door Leaf Process
Doo Leaf Nailing

## Slide 12
Door Core Lamination
(cold press)
Veneer Lipping
Solid Wood Eadge Lipping

## Slide 13
It is mainly used for the workpiece to be automatically moved to the conveying and turning after being edge-sealed. Whether the workpiece is longitudinal or horizontal, it can be automatically rotated to the feeding end.
Auto Reversal Edge-sealed Production Line：

## Slide 14
Double-sided Auto Sanding Production Line
One part of the machine is a down-press type, another is a floating type, and the double-side sanding is completed at one time, which can greatly improve the sanding precision, up to 0.20mm. The accuracy determines the speed. Only the good sanding effect can improve the quality of the roller coating, the processing efficiency and the product quality.

## Slide 15
Auto Door Leaf Production Line
Integrated with the process of laminating, cutting, edge bonding and punching. Available for sealing with the solid wood, veneer and PVC edge rubber. This three-purpose door production line is currently the first in China.

## Slide 16
Punching
Holes are punched in the upper and lower ends of the door leaf through the production line to facilitate the conveying and other processes such as painting.

## Slide 17
Carving
Highlighting the 3D effect, the plane products are machine-carved and the intricate pattern products are hand-carved.

## Slide 18
Nailing
Process after Sanding.
The well painted battens are directly pressed on the door frame with the nail-free glue. The overall paint of the product is adjusted and assembled after the bulk parts are painted, which reduces the nails and the scar, makes the paint surface clean, polish smoothly and improves the quality of the detail joggle.

## Slide 19
Batten Pressing Machine
The machine is mainly used for nailing. Some molding parts on the surface of the frame are nailed to the top of the product and placed into the machine smoothly. The process takes 10-15 minutes.

## Slide 20
Itatian Membrane Press
The double-sided membrane press which imported from Italy is the soul equipment of the solid wood moulding door workshop. It costs more than 220 thousand US dollars, and it can complete the double-sided large-area and large-drop shaped veneer within 4 minutes.

## Slide 21
Hardware Hole Processing
According to the hardware drawing, the hole position and the hinge position are respectively opened. The door is aligned with the hole of the door frame to ensure a 3 mm gap around the door leaf.

## Slide 22
Door Quality Inspection
1. Check the door frame & leaf thickness with a micrometer, tolerance ±1.0mm.
2. Measure with tape, door frame height and width tolerance are within +3.0mm and +1.5mm. Door leaf height and width tolerance are within -1.5mm and -3.0mm.
3. Measure the interior angle of the door frame, exterior angle of the door leaf. The diagonal length tolerance is within 3.0 mm.

## Slide 23
C. Door Frame Process
Pressing of Door Frame
Evenly gluing the surface and side of the core material;；
After processing, the tolerance of the periphery is within ±0.5mm, and the surface is intact and no delamination.

## Slide 24
Door Frame Painting
Apply waterproof paint to the baseboard of the door frame, which can prevent the influence of wall humidity when the wooden door is installed on site.
Door Frame Veneering
Door Frame Sawing
Door Frame Length Fixing
Cut the material according to wall thickness of the order.
Cut according to the actual length of the door frame.

## Slide 25
Architrave Mortise and Tenon
Sanding and Thickness Fixing
Pin Board
Architrave Matching

## Slide 26
Architrave Shaping
Sanding and Finishing
Veneer Matching
Veneer Trimming
Veneer Laminating

## Slide 27
D. Painting Process
After the upgrade, power loss is 80 KHW less than the previous mercury lamp, which avoids the pollution of the mercury lamp, ozone free, improves the production environment, greatly reduces the rework rate, makes the product more stable, does not affect the original design, and the instant drying low temperature which can meet more coating effect, saving two-thirds of the paint amount. The comprehensive production capacity is tripled, greatly reduces the cost, saving energy, greener and more efficient.
LED-UV Primer Roller Painting Line

## Slide 28
Infrared induction spray, injection stops after the product is delivered.Compared with the traditional injection, saves two-thirds of the paint, while reducing the power consumption by 50 KWH, paint can be recycled. Compared with the roller painting line, it can spray shaped products. After the LED-UV reciprocating spraying machine, the grinding efficiency is higher, thus achieves quick drying, environmentally friendly and energy saving.
LED-UV Reciprocating Spraying Line

## Slide 29
Sandpaper is used to make the surface of the paint smoother.
The difficulty of sanding is the angle of the product, the lines and the edges of the lines. One door leaf should be polished about 5 times, each time takes 20-30 minutes.
Paint Polishing
Match the color paste same as the swatch and spray it on the product to make the color consistent.
Shading

## Slide 30
Spraying Machine
This equipment works with the dust-free painting room especially for the finish paint to ensure the paint surface smooth and spotless.
Sanding

## Slide 31
Electrostatic Spray Coating Renovation
1
2
3
4
High efficiency.
High painting rate, less waste, costs only 50% of the previous air spray gun.
Environmentally friendly.
The paint surface is more even.
Four Advantages

## Slide 32
4 Core
Tech
1. The imported 100,000 rpm/min high-speed rotary cup spray gun, with good spray atomization, particle size is only one-fiftieth of the normal air spray gun.
2. The precision gear pump oil supply system is better and more stable than the gas pump.
3. The segmented fuel injection control system can effectively solve the problem of paint sag during hanging spray.
4. Infrared senses the size of the workpiece and intelligently adjusts the spray range.
Large Carriers of Coating Industry
--Electrostatic Spraying

## Slide 33
E. Product Inspection
Product inspection requires the following tests:
1. Whether the company label and the order remarks are attached.
2. Check the size, type and customer information.
3. Check if the surface pitted and evenly.
4. Check if there are any scratches?

## Slide 34
F. Packaging
Door Frame Packing

## Slide 35
Door Leaf Packing
Mainly pack with cappers, infrared heat shrinking machines and others:
1. Door leaf packed with PU bag, foam on each side.
2. Sealing the PU bag.
3. Iron the PU bag smoothly with infrared heat shrinking machine.

## Slide 36
Steps:
1. Place the ironed product on the wrapper.
2. Put the corner guard.
3. Sealed the wrapper with scotch tape.
Door Leaf Packing

## Slide 37
Loading